CELL QUALIFICATION PROTOCOL

CYG-21700-50G  —  Cygnus Cell Technologies

| Document No. | CQP-CYG2170050G-00 |
| --- | --- |
| Target market | EU / UN-38.3 |

1. Purpose

This protocol defines the qualification testing of the CYG-21700-50G cell manufactured by Cygnus Cell Technologies, under IESF-4400. The cell is qualified across the following duty profiles: Automotive Traction  Grid Storage.

2. Scope

Applies to the 21700 cylindrical cell of chemistry NMC811 / Graphite-SiOx. Testing is performed by Northgate Cell Qualification Laboratory (NCQL).

3. Reference Documents

Test Method Procedure: Test Method Procedure — CYG-21700-50G

Acceptance Criteria  Limits: Acceptance Criteria  Limits (ACL) — CYG-21700-50G

Vendor datasheet: Cygnus Cell Technologies datasheet — CYG-21700-50G

4. Test Article Description

The following values are taken from the vendor datasheet.

| Manufacturer | Cygnus Cell Technologies |
| --- | --- |
| Cell format | 21700 cylindrical |
| Nominal voltage | 3.63 V |
| Charge voltage (max) | 4.20 V |
| Discharge cut-off (min) | 2.50 V |
| Rated capacity | 5.00 Ah |
| Storage condition | Store at 20 ÷ 5 °C and 30-50 % state of charge, in a dry area away from direct sunlight. |
| Supplied as | Supplied as 21700 cylindrical cells, 50 cells per transport tray. |

5. Conditioning and Test Window

Each cell is conditioned by CC-CV charge to 4.20 V and discharge to 2.50 V. Cells whose graded capacity falls outside the band 4.85 Ah to 5.05 Ah are rejected before testing.

6. Duty Profile Test Matrix

Table 1 — expands to one row per duty profile and conditioning rate.

| Sr. No. | Duty Profile | Conditioning Rate | Charge to | Discharge to | Cycles |
| --- | --- | --- | --- | --- | --- |
| 1 |  | 0.5C | 4.20 V | 2.50 V | 500 |
| 2 | Automotive Traction | 1.0C | 4.20 V | 2.50 V | 500 |
| 3 | Grid Storage | 0.5C | 4.20 V | 2.50 V | 500 |

7. Qualification Test Parameters

The block below is repeated for each duty profile. The placeholder row is replaced by one row per test taken from the ACL for that duty profile.

7.1 Qualification Tests — Automotive Traction

| Sr. No. | Test Parameter | Acceptance Limit | IESF-4400 Clause |
| --- | --- | --- | --- |
| 1 | Capacity Verification | ≥ 98.0 % of rated capacity at 0.5C, 25 °C * $ | §6.2 |
| 2 | DC Internal Resistance (DCIR) | ≤ 18 mΩ at 50 % SOC, 25 °C # | §6.3 |
| 3 | Cycle-Life Endurance | ≥ 80 % capacity retention after 500 cycles $ | §6.4 |
| 4 | Overcharge Tolerance | No fire, no explosion at 1.5 × V_max charge @ $ | §6.7 |
| 5 | External Short-Circuit | Case temperature ≤ 80 °C; no fire @ | §6.9 |
| 6 | Thermal Stability (Hot-Box) | No fire, no explosion after 130 °C / 30 min soak @ | §6.11 |
| 7 | Altitude Simulation | No leakage; ≤ 1.0 % capacity loss at 11.6 kPa / 6 h | §6.12 |

Acceptance Criteria:

All listed parameters meet the acceptance limits for this duty profile.

Conclusion:

The cell is qualified for this duty profile, subject to review.

7.2 Qualification Tests — Grid Storage

| Sr. No. | Test Parameter | Acceptance Limit | IESF-4400 Clause |
| --- | --- | --- | --- |
| 1 | Capacity Verification | ≥ 98.0 % of rated capacity at 0.5C, 25 °C (lot-acceptance) * $ | §6.2 |
| 2 | DC Internal Resistance (DCIR) | ≤ 18 mΩ at 50 % SOC, 25 °C # | §6.3 |
| 3 | Cycle-Life Endurance | ≥ 80 % capacity retention after 500 cycles $ | §6.4 |
| 4 | Overcharge Tolerance | No fire, no explosion at 1.5 × V_max charge @ $ | §6.7 |
| 5 | External Short-Circuit | Case temperature ≤ 80 °C; no fire @ | §6.9 |
| 6 | Thermal Stability (Hot-Box) | No fire, no explosion after 130 °C / 30 min soak @ | §6.11 |
| 7 | Altitude Simulation | No leakage; ≤ 1.0 % capacity loss at 11.6 kPa / 6 h | §6.12 |

Acceptance Criteria:

All listed parameters meet the acceptance limits for this duty profile.

Conclusion:

The cell is qualified for this duty profile, subject to review.

Applicable notes from the ACL:

* Capacity limits apply to graded cells only; ungraded cells are assessed per IESF-4400 §6.2.1.

# DCIR is measured by a 10 s DC pulse at 1.0C and corrected to 50% SOC.

@ Mechanical-abuse limits apply to cylindrical and prismatic formats; pouch cells are governed by Annex P.

$ The test voltage window is defined by the cell vendor datasheet electrical ratings, not by this table.

Revision Record

This table is completed manually and MUST remain blank at issue.

| Revision | Date | Description | Author |
| --- | --- | --- | --- |
| 00 |  |  |  |