CELL QUALIFICATION PROTOCOL

PLX-PCH-088  —  Pollux Power

| Document No. | CQP-PLXPCH088-00 |
| --- | --- |
| Target market | Global |

1. Purpose

This protocol defines the qualification testing of the PLX-PCH-088 cell manufactured by Pollux Power, under IESF-4400. The cell is qualified across the following duty profiles: Automotive Traction  Grid Storage  Consumer Electronics.

2. Scope

Applies to the pouch cell of chemistry NMC622 / Graphite. Testing is performed by Northgate Cell Qualification Laboratory (NCQL).

3. Reference Documents

Test Method Procedure: Test Method Procedure — PLX-PCH-088

Acceptance Criteria  Limits: Acceptance Criteria  Limits (ACL) — PLX-PCH-088

Vendor datasheet: Pollux Power datasheet — PLX-PCH-088

4. Test Article Description

The following values are taken from the vendor datasheet.

| Manufacturer | Pollux Power |
| --- | --- |
| Cell format | pouch |
| Nominal voltage | 3.70 V |
| Charge voltage (max) | 4.20 V |
| Discharge cut-off (min) | 2.80 V |
| Rated capacity | 8.80 Ah |
| Storage condition | Keep at 15-25 °C, 30 % SOC. |
| Supplied as | Provided as single-pouch cells in anti-static sleeves, 20 per carton. |

5. Conditioning and Test Window

Each cell is conditioned by CC-CV charge to 4.20 V and discharge to 2.80 V. Cells whose graded capacity falls outside the band 8.55 Ah to 8.95 Ah are rejected before testing.

6. Duty Profile Test Matrix

Table 1 — expands to one row per duty profile and conditioning rate.

| Sr. No. | Duty Profile | Conditioning Rate | Charge to | Discharge to | Cycles |
| --- | --- | --- | --- | --- | --- |
| 1 |  | 0.5C | 4.20 V | 2.80 V | 500 |
| 2 | Automotive Traction | 1.0C | 4.20 V | 2.80 V | 500 |
| 3 | Grid Storage | 0.5C | 4.20 V | 2.80 V | 500 |
| 4 |  | 0.7C | 4.20 V | 2.80 V | 500 |
| 5 | Consumer Electronics | 1.0C | 4.20 V | 2.80 V | 500 |

7. Qualification Test Parameters

The block below is repeated for each duty profile. The placeholder row is replaced by one row per test taken from the ACL for that duty profile.

7.1 Qualification Tests — Automotive Traction

| Sr. No. | Test Parameter | Acceptance Limit | IESF-4400 Clause |
| --- | --- | --- | --- |
| 1 | Capacity Verification | ≥ 98.0 % of rated capacity at 0.5C, 25 °C * $ | §6.2 |
| 2 | DC Internal Resistance (DCIR) | ≤ 18 mΩ at 50 % SOC, 25 °C # | §6.3 |
| 3 | Cycle-Life Endurance | ≥ 80 % capacity retention after 500 cycles $ | §6.4 |
| 4 | Insulation Resistance | ≥ 100 MΩ at 500 V DC | §6.5 |
| 5 | Overcharge Tolerance | No fire, no explosion at 1.5 × V_max charge @ $ | §6.7 |
| 6 | Forced Over-Discharge | No fire, no explosion; cell reversal limited to −0.50 V @ | §6.8 |
| 7 | External Short-Circuit | Case temperature ≤ 75 °C; no fire, no rupture @ | §6.9 |
| 8 | Thermal Stability (Hot-Box) | No fire, no explosion after 130 °C / 30 min soak @ | §6.11 |
| 9 | Altitude Simulation | No leakage; ≤ 1.0 % capacity loss at 11.6 kPa / 6 h | §6.12 |

Acceptance Criteria:

All listed parameters meet the acceptance limits for this duty profile.

Conclusion:

The cell is qualified for this duty profile, subject to review.

7.2 Qualification Tests — Grid Storage

| Sr. No. | Test Parameter | Acceptance Limit | IESF-4400 Clause |
| --- | --- | --- | --- |
| 1 | Capacity Verification | ≥ 98.0 % of rated capacity at 0.5C, 25 °C (lot-acceptance) * $ | §6.2 |
| 2 | DC Internal Resistance (DCIR) | ≤ 18 mΩ at 50 % SOC, 25 °C # | §6.3 |
| 3 | Cycle-Life Endurance | ≥ 80 % capacity retention after 500 cycles $ | §6.4 |
| 4 | Insulation Resistance | ≥ 100 MΩ at 500 V DC | §6.5 |
| 5 | Overcharge Tolerance | No fire, no explosion at 1.5 × V_max charge @ $ | §6.7 |
| 6 | Forced Over-Discharge | No fire, no explosion; cell reversal limited to −0.50 V @ | §6.8 |
| 7 | External Short-Circuit | Case temperature ≤ 75 °C; no fire, no rupture @ | §6.9 |
| 8 | Thermal Stability (Hot-Box) | No fire, no explosion after 130 °C / 30 min soak @ | §6.11 |
| 9 | Altitude Simulation | No leakage; ≤ 1.0 % capacity loss at 11.6 kPa / 6 h | §6.12 |

Acceptance Criteria:

All listed parameters meet the acceptance limits for this duty profile.

Conclusion:

The cell is qualified for this duty profile, subject to review.

7.3 Qualification Tests — Consumer Electronics

| Sr. No. | Test Parameter | Acceptance Limit | IESF-4400 Clause |
| --- | --- | --- | --- |
| 1 | Capacity Verification | ≥ 98.0 % of rated capacity at 0.5C, 25 °C (field-return cells: ≥ 96.0 %) * $ | §6.2 |
| 2 | DC Internal Resistance (DCIR) | ≤ 18 mΩ at 50 % SOC, 25 °C # | §6.3 |
| 3 | Cycle-Life Endurance | ≥ 80 % capacity retention after 500 cycles $ | §6.4 |
| 4 | Insulation Resistance | ≥ 100 MΩ at 500 V DC | §6.5 |
| 5 | Overcharge Tolerance | No fire, no explosion at 1.5 × V_max charge @ $ | §6.7 |
| 6 | Forced Over-Discharge | No fire, no explosion; cell reversal limited to −0.50 V @ | §6.8 |
| 7 | External Short-Circuit | Case temperature ≤ 75 °C; no fire, no rupture @ | §6.9 |
| 8 | Thermal Stability (Hot-Box) | No fire, no explosion after 130 °C / 30 min soak @ | §6.11 |
| 9 | Altitude Simulation | No leakage; ≤ 1.0 % capacity loss at 11.6 kPa / 6 h | §6.12 |

Acceptance Criteria:

All listed parameters meet the acceptance limits for this duty profile.

Conclusion:

The cell is qualified for this duty profile, subject to review.

Applicable notes from the ACL:

* Capacity limits apply to graded cells only; ungraded cells are assessed per IESF-4400 §6.2.1.

# DCIR is measured by a 10 s DC pulse at 1.0C and corrected to 50% SOC.

@ Mechanical-abuse limits apply to cylindrical and prismatic formats; pouch cells are governed by Annex P.

$ The test voltage window is defined by the cell vendor datasheet electrical ratings, not by this table.

Revision Record

This table is completed manually and MUST remain blank at issue.

| Revision | Date | Description | Author |
| --- | --- | --- | --- |
| 00 |  |  |  |